ARC WELDING NOTES

ARC WELDING – Shielded Metal Arc Welding (SMAW). Electricity, as it jumps a gaseous gap between two conductors. Produces an arc as intense as 9000( F.

TYPEs OF WELDERS

Rectifier

D.C. (Direct Current) – Electricity is converted from A.C. (Alternating Current) through transformers and rectifiers.

# A.C. / D.C. – Dual purpose

ELECTRODES

Usually 14” long

- 1 -Classification – Brand names differ but the A.W.S. number system is the standard:

Example = E6013 = E  XXXX

E = Electrode

60 = Tensile strength X 1000 psi

1 = Rod position (1 = all, 2 = horizontal or flat, 3 = flat only)

3 = Dealer characteristics – polarity, application, flux,

composition, etc.

## FIVE FUNCTIONS OF FLUX/SLAG

- Cleans metal of oxides	2. Stabilizes the arc

3.  Keeps oxygen away		4. Forms the weld

- Lets the weld cool slowly

POLARITIES

1.  Direct current straight polarity – (D.C.S. P.)

2.  Direct Current Reverse Polarity – (D.C.R.P.)

# DCRP flows in one direction also (- to +) but the leads are reversed.

# 1/3 heat at the base

# and 2/3 heat at the rod.

# Characteristics

- Deep penetration –

good for thick metals

- Prone to arc blow

- Alternating Current - (A.C.)

STRIKING AN ARC – Like striking a match – touch the electrode to the metal, then circle up and back down to the dia. of the rod away from the base metal.

Motion -  (Avoid excessive movement)

A. Straight -  			Feed in & drag the puddle

ROD POSITION

# Flat – Rod perpendicular to base metal. Incline about 20( from perpendicular toward direction of travel. Drag the weld. (Backhand)

# Lapp or Inside Corner – Angle rod 30( to 45( to base metal. Incline 20( toward direction of travel. Drag weld.

WELD JOINTS

Butt joint – prepare joint. Metal must be clean. Always tack & vee thick pieces for penetration. Use a slight motion back & forth.

Flange (edge joint) – Always tack. Easiest weld. Thick pieces should be veed.

Lapp joint – Very common. Plug, rosette, slot welds are all variations of the lap weld. Concentrate heat on bottom plate. Use a slight weave motion. Always tack.

Inside Corner (Tee joint) – Equal weld on each plate. Finished joint should be concave to flat. Use a close arc. Concentrate heat on bottom plate. Always tack.

Outside joint – Allow for natural vee. Always tack. Use a slight weave.

WELDING POSITIONS

Flat

Horizontal (on a vertical plane).

Vertical

Overhead

PROBLEMS

Arc Blow –

# A magnetic force deflects the weld into splitting.

# Cure – Reestablish ground. Shorten arc length.

Undercut

# A trough or erosion cut on

# either side of the weld.

# Cure – Turn down heat or shorten arc length or hesitate at the edges to fill in.

Rod Sticks

# Break the circuit or current . Release electrode from the electrode holder.

# Cure/Cause – Too cold heat setting, too close, not striking it, wrong electrode or wrong polarity.

Arc Won’t Start

# Check out the following

Machine set up and switches

Check for proper ground

Check rod – held in stinger, end glassed over.

Welds

# Splits – mistaken for arc blow –

# moving rod too fast.

# Go slower to let it fill in with filler rod.

SAFETY

Protective equipment – All the listed equipment protects you from heat, splatter and harmful rays. (Ultraviolet & Infrared).

# Gloves – leather

Do not hold hot metal or get them wet. Leather shrinks, burns and hardens.

# Jacket – leather

Not to be used as a shop coat. For arc welding only.

# Helmet – A full head and face shield

Protects head, face, and neck, can be adjusted and has a #10 welding lens.

NEVER…

# Expose skin or eyes to a flash or arc.

# Misuse equipment – change the amperage setting on the machine while under a load or during the welding process.

# Chip slag without eye protection.

# Take a chance with electricity.

# Weld on the table, booth or anything that is not a project.

# Exceed the welder’s Duty Cycle – the amount of time the machine can work before it needs to cool down.

Example: 70% Duty Cycle at 150 amps = You can weld 7 out of 10 minutes. The duty cycle is 10 minutes from when you start and continues in 10 minute blocks from there on.